FORM MRPL-NDT-04: Statutory Vessel Inspection & Technical Approval Note

Equipment Tag: Crude Distillation Column Vessel V-1001 (CDU-II)

| Technical Parameter | Recorded Value |
| --- | --- |
| Material | Carbon Steel SA-516 Gr 70 |
| Nominal Thickness | 14.0 mm |
| Minimum Design Thickness (t_min) | 9.5 mm |
| Critical Measured Thickness | 11.2 mm (Tray #14 Feed Nozzle) |
| Corrosion Rate | 0.12 mm/year |
| Remaining Life | 14.16 years = (11.2 − 9.5) / 0.12 |

## Statutory Compliance Matrix

| Requirement | Reference | Assessment | Status |
| --- | --- | --- | --- |
| Inspection criteria | OISD-STD-117 §4.3 | Remaining corrosion life reviewed | COMPLIANT |
| Pressure vessel code | IS 2825:1969 §6.1 | Inspection record cross-checked | COMPLIANT |
| In-service inspection | API 510 §6.4 | Thickness trend reviewed | COMPLIANT |

## Recommendation

A 36-month service extension is recorded in this mock assessment, through September 2029, subject to applicable statutory approvals and plant authorization.

## Sign-off

| Role | Name / ID | Signature / Hash |
| --- | --- | --- |
| Senior Quality Inspector | Rina Sharma / MRPL/QI/2891 | DIGITAL HASH: DEMO-7A91-C2 |
| Chief Process Manager | Dev Nair / MRPL/PE/1247 | DIGITAL HASH: DEMO-9F31-K8 |